DEPARTMENT OF CIVIL ENGINEERING EASTERN MEDITERRANEAN UNIVERSITY HIGHEST CONCRETE STRENGTH COMPETITION 2026

1.   INFORMATION ABOUT CEMENT

Cement available for making concrete sample is BEM 42,5 R.

2.   INFORMATION ABOUT AGGREGATES

| Physical properties of aggregates. |  |  |
| --- | --- | --- |
| Physical properties | Fine aggregate | Coarse aggregate |
| Relative Density (Saturated surface dry) | 2.76 | 2.74 |
| Relative Density Oven Dry | 2.68 | 2.70 |
| Apparent Relative Density | 2.92 | 2.81 |
| Water absorption | 3.09% | 1.39% |